1. Introduction

Inverse adding-doubling is a method for generating the optical properties of scattering and absorbing materials. Reflection and transmission measurements are converted to the optical properties of the sample using the IAD.

2. Testing

prompt> iad -v

validate by running the valid.bat file

not sure about the make condition

3. Experimental Decision

To get the optical properties µa, µa-1 , MR, MT, and δ have to measure and the anisotropy is fixed (default g = 0)

The iad require that the total reflection MR  and MR be measured. (do not need to decide if the unscattered reflection or unscattered transmission should be included)

Always placed the baffle between the sample and the detector

The corrections needed for the sphere are least at the two ends and highest in the center.

To minimize the need for these corrections, it is best to use a reflective standard that is slightly higher than all the sample parameters.

# the index of refraction of polyurethane is n = 1.5. the reflectance of the sample will be at least 4% due to specular reflectance. There measurements only give 3%

The sphere efficiency (gain) was so high, the calculation value of MR could be 25% lower.

The sample area to be not more than 10% of the sphere wall area.

The sample size

Have large aspect ratios for the sample (port diameter is ten times the sample thickness)

A beam 1 mm in diameter, a sample 1 mm thick, a port 10 mm in diameter, and a sphere 100 mm in diameter are all reasonable.

Sample diameter should be larger than the sample size.

# data file

The basic structure of the data file consists of a header section followed by your measurements of reflectance and transmittance.

The header section

The sample thickness

The beam diameter

The indices of refraction,

The number and geometry of the spheres used.

When using the one reflectance sphere

The entrance port diameter is defined as the size of the port though which light enters the sphere.

The sample port is the size of the hole in the sphere that is adjacent to the sample.

The detector port diameter is the size of the port that housed the detector or optical fiber.

Measurements were conducted using an 850 nm nominal IR laser module (Egismos S8), with a measured peak emission at 852 nm. The system was calibrated against a NIST-traceable PTFE standard with 99.3% reflectance at the operating wavelength.

Beam size 15 mm round at 3m,

15x30mm at 10m