## Slide 1
Presentation XIII
Thu Ta Zaw
2415121095
  Bone Tissue Phantom

## Slide 2
  Preliminary Measurement of PLA optical properties
Table. Preliminary Measurement Result of PLA
  The reduced scattering coefficient is within the range of the standard PLA.
  The absorption coefficient is overestimated when compared to the standard PLA.
  However, both value are acceptable upon comparing with the human bone.

## Slide 3
  Optical Properties on Bone Analysis: An Approach to Biomaterials
  Perform the measurement of the optical properties of chicken femoral samples.
  Used the sample thickness of 3 mm.
  Optical Properties on Bone Analysis: An Approach to Biomaterials
  The total transmittance and reflectance measurements were performed I the 800-2000 nm wavelength range using the commercially available spectrometer with integrating sphere.
  The thickness of the samples varied from 2.0±0.1 to 5.0±0.5 mm.
  Specimens size for Integrating Sphere Measurement

## Slide 4
  Effect of light losses sample between two integrating spheres on optical properties estimation
  When the size of the integrating sphere port is constant, the dependence of the error on the thickness of the sample is discussed.
  The thicker the sample, the larger the error of the optical property estimation is.
  The difference of error caused by the change in thickness of the sample is very tiny
  Specimens size for Integrating Sphere Measurement
Sample Thickness | Max Light Loss (Aiad/A0) | Max Absorption Error (µa)
0.7 mm | 125 % | 17%
0.8 mm | ~126-127 % | 18%
0.9 mm | 128 % | 19%
Table. Summary of thickness related error.

## Slide 5
  Ex Vivo Optical Properties Estimation for Reliable Tissue Characterization
    The size of the sample should be slightly larger than the size of the port diameter ensuring the sample completely covers the port to prevent light leakage.
      Freshly excised biological samples representing soft and thin tissues (skin, skull, liver and muscle) were used with size of (2x2 ).
    For the thickness, samples should keep thin, typically under 3 mm, to avoid significant beam displacement during transmittance measurements.
      The thickness of each samples is 3 mm.
  Specimens size for Integrating Sphere Measurement
Table. Ports size of the ND-Seiko Integrating sphere

## Slide 6
    The recommend size for the specimen is (32Dx2) mm or (32x32x2) mm
  Specimens size for Integrating Sphere Measurement
Fig. 32x2 mm sample side view and front view
Fig. 2 mm sample holder

## Slide 7
  Phantom for standardization in functional near-infrared spectroscopy, optical properties and Monte Carlo simulations
      The international standard IEC 80601-2-71 defines requirements for the basic safety and essential performance of medical continuous wave functional near-infrared spectroscopy (fNIRS) equipment.
      The POM-C matrix exhibits negligible absorption and monotonically decreasing reduced scattering coefficient from (10.5 down to 8.5 cm-1) in the 650 to 850 nm range.
      Manufacturer is Duracon NE25X, Polyplastics, Tokyo, Japan).
  Validation For Integrating Sphere
Table. Optical properties of the POM-C

## Slide 8
  [3] Optical characterization of 3D printed PLA and ABS filaments for diffuse optics applications [extinction coefficient]
      White ABS at this wavelength is more opaque than PLA due to its higher pigment loading and base polymer density.
      Since the absorption coefficient (µa) at his coefficient is nearly zero, the measurement will primarily validate the scattering coefficient (µs).
  Validation For Integrating Sphere
Table. Expected Transmittance for white ABS and PLA
Material | µ at 850 nm (cm-1) | Expected Transmittance (T)
White PLA | ~62.5 | 4.4%
White ABS | ~92.0 | 1.0%

## Slide 9
  Polydimethylsiloxane tissue-mimicking phantoms with tunable optical properties
  PDMS is optically transparent in VIS-NIR.
  It has no fluorescence background.
  It has long-term mechanical and optical stability.
  I can be easily moldable into solid phantoms.
  Its refractive index is similar to biological tissue ().
  Its absorption and scattering coefficients can be tuned independently by adjusting the concentration of Carbon black powder (strong broadband absorber) and Titanium dioxide (efficient elastic scatter).
  (w/w) curing reagent is added into the mixture to solidified the PDMS.
  Validation For Integrating Sphere
A step-by-step phantom fabrication procedure

## Slide 10
  Three-dimensional printed optical phantoms with customized absorption and scattering properties
    Commercially available thermoplastics provide only a small range of physiologically relevant absorption coefficient (µa)and reduced scattering coefficient (µs’) values.
    The object of this research is to fabricate and validate customizable acrylonitrile butadiene styrene (ABS) filaments for dual extrusion 3D printing of tissue mimicking optical phantoms.
    µa and µs’ values were adjustable by incorporating nigrosine and titanium dioxide in the filament extrusion process.
    A wide range of physiologically relevant properties was demonstrated with average repeatability with 11.5% for µa and 7.71% for µs’ .
    Advantages
      3D printing with user defined optical properties may provide a viable method for durable optically diffusive phantoms for instrument characterization and calibration.
      Can mitigate the problem of Liquid phantoms and solidified materials often limiting the ability to control the geometry of the final product.
  3D printed ABS Optical Bone Phantom

## Slide 11
  Three-dimensional printed optical phantoms with customized absorption and scattering properties
    A key step to improving the versatility of 3D printed optical phantoms is the ability to alter the raw materials’ intrinsic optical properties to match that of a know target tissue.
    The methodology to customized optical phantoms is the addition of absorbing dye, nigrosine, and scattering agent, titanium dioxide TiO2 , prior to extrusion.
  3D printed ABS Optical Bone Phantom
Table 1: Mean ± standard deviation µa and µs’ values for all cubs at 471 nm.
Fig. White light image (left), and SFDI maps of absorption (middle)
and reduced scattering (right) at 471 nm.

## Slide 12
  Development of a composite using calcined bone powder and silane cross-linked alginate as bone substitute material
  3D printed ABS Optical Bone Phantom
Fig. Absorption, averaged overall TiO2 concentrations, and reduced scattering, averaged overall nigrosine concentration
of all 3D printed cubes for 471,526,591,621,659,691,731
    Absorption coefficient of human bone (µa) : 0.01 – 0.05 mm-1
    Scattering coefficient of human bone (µa) : 20 – 45 mm-1
    Reduced Scattering coefficient of human bone (µa) : 2.0 – 4.5 mm-1

## Slide 13
  Development of a composite using calcined bone powder and silane cross-linked alginate as bone substitute material
  Filament preparation
    Co-extruding a mixture of commercially available natural color ABS pellets with custom absorption and scattering ABS “chips”. (combining ABS with either nigrosine and TiO2)
    Fabrication of TiO2 chip consisted with dissolving the 20g of ABS in 50 ml of acetone for at least 12 hours. 0.2 g of TiO2 was mixed with 1000 µl of water and sonicated for 10 minutes. After that add to the ABS solution. The mixture was then poured into a 21x21 cm pan to a layer thickness of 1.5 mm and vacuumed to remove air bubbles. The pan consisting of ABS/TiO2 solution were left in the 40 kPa vacuum overnight to dry and solidify. Once it is solidified the thin sheet is cut into 2 x 2 mm dimension.
  3D printed ABS Optical Bone Phantom

## Slide 14
  Development of a composite using calcined bone powder and silane cross-linked alginate as bone substitute material
  Filament preparation
    The nigrosine chips were also created using the same protocol described above by using the 0.02g of nigrosine and 800 µl of water.
    Nigrosin and TiO2 chips were mixed together prior to extrusion in the desired mass ratio and added to the hopper throughout the extrusion process to provide a more homogeneous filament product.
    30 g batch of raw ABS pellets and chips yielded approximately two 2x2x2 cm 3D printed cubes.
  3D printed ABS Optical Bone Phantom

## Slide 15
  In this study, the ultimate tensile strength was modified by blending different ratio of PLA and PCL resulting in an optimum value of approximately 30 MPa when the ratio of PLA to PCL reached 3:1.
  It is observed that the addition of 1% TiO2 to the immiscible PLA/PCL composite increase in the tensile strength up to 37 MPa.
  Upon examining the biocompatibility of PLA/PCL/TiO2 composite, vigorous cell growth was observed.
  The final composite has a comparable mechanical strength of the ideal cancellous bone structure.
  Characterization of 3D printed PLA/PCL/TiO2 Composites for Cancellous Bone
Fig. 3D printed model of cancellous bone with PLA/PCL/TiO2 composite

## Slide 16
  PLA is cheaper option to make the bone graft as the process of grafting is expensive using metal is expensive, and it can reduce the problems related to metal’s higher strength (stress shielding) and toxicity.
  As PLA and PCL are synthetic biodegradable thermoplastic polymer, it is compatible to use with human body and TiO2 is an inorganic particle exhibiting suitable biocompatibility and it is well-known for non-toxic depending on size of the particle and condition of aggregation.
  The Materials used in the study are as followed:
    The Polylactic acid (PLA) was a commercial grade with density of 1.24 g/cc.
    The Polycaprolactone (PLC) has a density of 1.15 g/cc.
    TiO2 has a density of 4.26 g/cc.
  Characterization of 3D printed PLA/PCL/TiO2 Composites for Cancellous Bone

## Slide 17
  Filament Preparation
    To make the filament, a blend was prepared to make pellets with the desired composition.
    The first blends made were a mixture of PLA/PCL with different composition (75/25, 50/50, 25/75 wt%).
    The mixing process starts by first melting the corresponding amount of PLA due to its higher melting point. PCL is then added and when the blend is uniformly mixed, the filler is added and stirred until a homogeneous mixture is achieved.
    The blend of the PLA/PCL 75/25 wt% showed the best characteristics and add the 1 wt% TiO2 to the ratio.
  Characterization of 3D printed PLA/PCL/TiO2 Composites for Cancellous Bone

## Slide 18
The End
THANK YOU FOR LISTENING
Thu Ta Zaw
2415121095