OPTICAL PROPERTY-BASED SELECTION OF HUMAN BONE PHANTOMS AT 850 NM USING INTEGRATING SPHERE MEASUREMENTS AND THE INVERSE-ADDING-DOUBLING METHOD.

# CHAPTER 1	 INTRODUCTION

## 1.1 Introduction

Near-infrared (NIR) optical region (700-2500 nm) has been interested in biomedical diagnostics, and tissue characterization due to their ability to penetrate biological tissues with relatively low absorption. The characterization of optical properties of different types of tissue in these wavelengths has been done in recent years. Among the wavelengths, 850 nm is widely used in many diagnostic and monitoring systems such as diffuse optical spectroscopy, photo biomodulation systems, and brain functional monitoring systems as it has a balance between scattering and absorption [1,2, paper for adv of 850 nm]. It is therefore important to characterize the tissue intrinsic optical properties at this wavelength for accurate system calibration, computational modeling, and experimental validation.

Intrinsic optical properties determine the light propagation in biological tissues which determine photon attenuation, diffusion behavior, penetration depth, and spatial reflectance distribution. Due to multiple scattering events taken placed in tissues, it is difficult to conduct analytical measurements of these intrinsic optical properties. Therefore, it is necessary to perform experimental measurements combined with inverse computational modeling to determine the intrinsic optical coefficients [1,3, difficult to measure mentioned paper].

Measurement of total diffuse reflectance, R, and total diffuse transmittance, T, from turbid media can be done by various methods including single and double integrating sphere methods which can minimize angular bias and enable accurate macroscopic characterization of optical behavior [3,papers in iad]. However, these measurements cannot directly give intrinsic optical properties and inverse modeling approaches are required. There are many inverse modeling techniques including diffusion approximation, Monte Carlo photon transport simulation and Inverse Adding-Doubling (IAD) method. Among them IAD is a widely recognized for its robustness and computational efficiency, which find the intrinsic optical properties by adjusting optical parameters until calculated reflectance and transmittance match experimental measurements iteratively [4,5,monte carlo, IAD papers]. Compared to diffusion approximation methods, IAD provides improved accuracy for highly scattering media and thin samples, and it is more computationally efficient than Monte Carlo simulation while providing a similar accuracy [IAD pharal paper].

Since human bones exhibit strong scattering due to its composition, pervious studies [6,7 from intro,and paper in mote carlo] have reported that there are significant variations in bone optical properties depending on wavelength, anatomical location, and sample preparation. Therefore, wavelength specific measurements are required to provide accurate optical data for optical imaging and monitoring systems. As ethical and practical limitations are associated with human bone specimens, optical bone phantoms are favorable alternatives for using in calibration and experimental validation as they are engineered to replicate the absorption and scattering characteries of biological tissues [8 and PDMS paper]. However, the problem may arise while performing experiments and simulations as many phantom designs are based on assumed optical parameters. Therefore, phantom selection should be made based on the optical properties.

In this research, the selection of bone phantoms to use as human bone alternatives will be performed based on optical properties in which integrating measurements at 850 nm combined with the Inverse Adding-Doubling method which enhances reliability and reproducibility of the selection.

## 1.2 Objectives

- To experimentally acquire diffuse reflectance and transmittance data of PDMS-based bone phantoms at 850 nm using an integrating sphere.

- To extract intrinsic optical parameters (μₐ and μₛ′) via Inverse Adding-Doubling inversion.

- To establish an optical matching criterion by quantitatively comparing phantom parameters with human leg bone optical properties.

- To select the most optically equivalent phantom for subsequent biomedical optical applications.

## 1.3 Scopes

- To study the optical characterization at a single wavelength of 850nm in the near-infrared NIR region

- To perform optical measurements at steady-state.

- To investigate the intrinsic optical parameters (Absorption coefficient and reduced scattering coefficient) of the bone phantom.

- To measure the diffuse reflectance (R) and total transmittance (T) are measured using a single integrating sphere system.

- To Calibrate the optical measurement system using the reference standards.

- To perform the background and dark signal correction for the detector.

- To perform measurement on the thickness-controlled phantom samples.

- To compare the intrinsic optical properties of bone tissue phantoms with published human bone studies values.

- To select the suitable PDMS-based bone phantoms for the human bone optical studies.

## 1.4 Expected Benefits

- Improves the reliability of bone phantom selection through quantitative optical-property matching rather than assumption-based design approaches.

- Enables the development of optically equivalent PDMS-based bone phantoms for controlled biomedical optical experiments at 850 nm.

- Provides reusable, stable, and tunable phantom materials, ensuring consistent experimental conditions and repeatability.

- Reduces dependence on real human bone samples, supporting ethical research practices and improving experimental accessibility.